## Slide 1: Photocatalytic Water Splitting
——表面物理第一小组

## Slide 2: Outline
Introduction
The basic mechanism
Photolysis in TiO2
Optimization for photocatalytic activity
Conclusion

## Slide 3: Introduction
Why Photocatalytic water splitting?
Water splitting:
  : clean fuel——no pollution or green-house effect gas.
  “”: water/air purification——degrade and mineralize organics into and harmless inorganic anions.
  The principle may be used to make primary battery.
Photo: convert solar energy into chemical energy
  Renewable
  Environment friendly
  Economic

## Slide 4
For electrochemical decomposition of water, a potential difference more than 1.23V is needed.
This is equivalent to a photon of nm (infrared light).
However, this reaction is kinetically very slow for380 nm.
Due to the transparency of water to visible light, photolysis can only occur with 180 nm.
The photocatalysts are needed!

## Slide 5: The basic mechanism
Main processes of photocatalytic water splitting:

## Slide 6
Requirements for photocatalysts
Difficulty to overcome
  Recombination of pair
  Fast drawback reaction
  Inability to utilize visible light
  Catalyst decay
Notes: 在太阳光中，可见光占很大一部分能量

## Slide 7: Photolysis in TiO2
Advantages:
  strong catalytic activity
  high chemical stability (non-corrosive)
  long lifetime of electron/hole pairs
  Environmentally friendly
  Abundant and cost effective.
Honda–Fujishima effect
Pt counter electrode
TiO2 n-type photoelectrode
Notes: 最早实现；被广泛的研究。

## Slide 8: Optimization
Difficulty and possible solution
  Recombination of pair:
    Co-catalyst to separate electron and holes
    Chemical addition—electron/hole doner
    Atomic layer deposition (ALD)—passivate surface states
  Fast drawback reaction
    Chemical addition
  Inability to utilize visible light
    Dye sensitization
    Composition Semiconductor
  Catalyst decay
    Atomic layer deposition
Notes: 应用——优化
水的光解包括产氢，产氧和全分解。这里主要介绍关于产氢的方法。
在全分解中，产氧为控速步骤。

## Slide 9: Co-catalyst: Noble metal loading
The Fermi levels of some noble metals (Pt, Au, Pd, Rh, Ni, Cu and Ag) are lower than that of TiO2.
Conduction band of TiO2 metal particles
Photo-generated holes remain on the valence band TiO2.
Reduce the possibility of recombination.
Drawback:
  Too much metal particle might reduce photon absorption by TiO2
  Become electron-hole recombination centers.
Dual cocatalysts: coloading of both H2/O2 evolution cocatalysts
Notes: 随着电子的转移金属的费米能级也被提高，进而可以催化产氢。
同时负载氢和氧可以进一步分离电子/空穴，提高反应效率

## Slide 10: Addition of electron donor(for H2)
Adding electron donors (sacrificial reagents or hole scavengers) to react irreversibly with the VB holes.
Organic compounds(hydrocarbons)
  Enhancement capability: EDTAmethanolethanollactic acid
  Decomposition of pollutants and production of clean hydrogen fuel
Inorganic ions
  IO3-/I-, S2-/SO23-and Ce4+/Ce3+……

## Slide 11: Z-scheme system
Semiconductors with suitable band positions are rare
Redox power is weakened by band-gap narrowing
A wider range of visible light utilization
Strong oxidation and reduction ability
Undesirable recombination of electrons and holes can be inhibited
The reverse reactions to regenerate H2O can be efﬁciently suppressed

## Slide 12: Atomic layer deposition
Theoretically, minimizing the particle of photocatalyst can reduce the time of electron/hole separation and increase the surface area and gas desorption.
Surface recombination and surface trapping states!
Hematite (-Fe2O3): inexpensive but large overpotential.
Current densities of the prepared photoanode
Broken lines: in dark
Solid line: under simulated solar illumination
Black: before ALD
Red: after ALD (Al2O3)
Green: annealing at 300 20 min
Blue: annealing at 400 20 min
Notes: 表面态的存在导致α-Fe2O3光电极拥有较大的反应过
电位

## Slide 13: Chemical addition: suppress backward reaction
Na2CO3 was found to be beneficial for hydrogen and oxygen production in various semiconductor photocatalysts.
holes were consumed to form carbonate radical.
Promote desorption of O2
minimize the formation of H2O from the backward reaction
Notes: 空穴和碳酸盐生成碳酸盐根阴离子自由基，促进电子空穴对分离
自由基生成氧气和二氧化碳，促进氧气的脱附，减少逆反应

## Slide 14: Dye sensitization
Dyes: redox property and visible light sensitivity
Efficient absorption of visible light and transfer of electrons from excited dyes to the CB of TiO2.
To regenerate dyes, redox systems or sacrificial agents are needed to sustain the reaction cycle.
Notes: 染料敏化

## Slide 15: Composite semiconductors
A large band gap semiconductor is coupled with a small band gap semiconductor.
Better charge separation.
Sacrificial agent has to be added

## Slide 16: Conclusion
The mechanism of photo-catalysis.
Strategies to improve photocatalytic activity:
  Enhancing visible light harvesting
  Boosting the separation and migration of photogenerated charge carriers
  Loading efficient cocatalysts for H2 and/or O2 evolution
Synergistic investigation of above strategies are needed.
Deeper understanding of the kinetics and dynamics of a photocatalytic reaction should is necessary to establish rational strategies.
Notes: 1.染料敏化 复合窄带半导体
2.复合半导体（分离电子空穴），改变反应过程（两个半反应）
3.助催化剂：贵金属等

## Slide 17: Thank you!